## Slide 1: Node names, FinFET → GAA
Week 1 · Why “3nm” isn’t 3 nm, how transistors wrapped the gate around the channel, and why power is moving to the back of the wafer
Notes: Welcome to week 1. Three ideas: node names are marketing, gate control drives transistor shape, and backside power is the next big structural change.

## Slide 2: What you’ll be able to explain
1
Node names
Why “3nm” is a brand and which metrics are real
2
Gate control
The electrostatics behind planar → FinFET → GAA
3
Nanosheet build
The process steps, and which ones are hard
4
Backside power
What moves under the wafer and what it changes
5
The 2nm race
TSMC, Intel and Samsung, through career and investor eyes
Notes: Roadmap for the week. Each item maps to a section of the written lesson and the podcast episode.

## Slide 3: “3nm” is a product name, not a measurement
3 nm
What the node is called
~15–20 nm
Typical gate length today
~48 nm
Gate pitch (CPP) of a 3nm-class node
28
20
16/14
10
7
5
3
2
Each step keeps the ~0.7× naming rhythm customers expect, even though no physical feature shrinks by that much.
Notes: Gate length stopped tracking node names in the late 1990s. Names kept the 0.7x cadence for marketing. Intel renamed its nodes in 2021 to line up with the industry.

## Slide 4: The numbers that actually describe a node
1
CPP
Contacted poly (gate) pitch: sets standard-cell width
2
MMP
Minimum metal pitch: sets cell height and routing
3
Cell height
tracks × MMP, e.g. 6 × 23 nm ≈ 138 nm
4
Logic density
MTr/mm², e.g. 0.6·NAND2 + 0.4·scan flip-flop
5
SRAM bit cell
µm² per 6T cell: barely shrinking lately
6
Cost & yield
$ per wafer and good dies per wafer decide everything
Notes: Compare nodes on pitches, density, SRAM cell area, performance per watt, yield and wafer cost, never on the name. SRAM scaling slowing down matters a lot for caches and AI chips.

## Slide 5: Pitches have nearly stopped shrinking
Chart: 
| Intel 22nm | Intel 14nm | TSMC N7 | TSMC N5 | TSMC N3E | TSMC N2 (est.)
Gate pitch (CPP, nm) | 90 | 70 | 57 | 51 | 48 | 45
Min metal pitch (MMP, nm) | 80 | 52 | 40 | 28 | 23 | 21
Read the chart
Gate pitch moved only ~6 nm from N5 to N2. Density still improves, mostly through DTCO tricks.
Approximate published and analyst figures; they vary by source and process variant.
Notes: Figures are rounded, approximate, and vary by source. The point is the trend: pitch scaling has slowed sharply, so density comes from design-technology co-optimisation.

## Slide 6: DTCO: smaller cells at the same pitch
7.5-track
6-track
5-track + backside power
Teal lines = routing tracks · Copper = power rails
Fewer tracks per cell: 9T → 7.5T → 6T → ~5T
Fin depopulation: 3 → 2 → 1 fin per device
Contact over active gate (COAG)
Single diffusion break at cell edges
Power rails moved under the cell, freeing tracks
Notes: Cell height equals tracks times metal pitch. Cutting tracks shrinks area even at constant pitch. Moving power rails to the back frees tracks in every cell.

## Slide 7: Gate control is everything
Why the transistor keeps changing shape
Notes: Section two: electrostatics.

## Slide 8: Short channels leak: wrap more gate around them
60 mV/dec
Ideal subthreshold swing at 300 K: (kT/q)·ln10
Natural length
λ ≈ √(ε_si · t_si · t_ox / (N · ε_ox))
Gate length should be several λ. N = gates around the channel.
1
Thinner body (t_si)
Fins, nanosheets, FD-SOI
2
Better dielectric (t_ox, ε)
High-k / metal gate since 45nm
3
More gates around channel (N)
1 → 3 → 4 sides: planar → FinFET → GAA
Notes: DIBL and Vt roll-off happen when the drain controls the channel. Swing worse than 60 mV per decade means more leakage or higher VDD. The levers are body thickness, dielectric, and number of gates.

## Slide 9: From planar to stacked: the gate wraps further
Planar
Gate on 1 side
to 28/20nm
FinFET
Gate on 3 sides
22nm (2011) → 3nm
GAA nanosheet
Gate on 4 sides
SF3 2022, N2, 18A
p
n
CFET
nFET stacked on pFET
Research, 2030s
Notes: Cross-sections looking down the channel. Copper is the gate, teal is the silicon channel, grey is the substrate. Each step wraps more gate around the channel. CFET stacks the p-type device over the n-type.

## Slide 10: Same footprint, but nanosheets can be sized freely
2-fin FinFET
W = fins × (2·H + W_fin)
= 2 × (2·50 + 6)
= 212 nm
Drive comes in whole fins only: 1, 2 or 3.
3-sheet nanosheet
W = sheets × 2·(W_sheet + T_sheet)
= 3 × 2·(30 + 5)
= 210 nm
Sheet width is a design choice: 15, 30 or 45 nm.
212 nm
FinFET effective width
210 nm
Nanosheet effective width
Notes: Worked exercise from the lesson. Raw width is similar. The real wins are better electrostatics and continuous sizing, which brings back analog-style transistor sizing for library designers.

## Slide 11: Building a nanosheet
Grow a layer cake, then carve the gate into it
Notes: Section three: process flow.

## Slide 12: Sacrificial SiGe makes room for the gate
1 · Grow Si / SiGe superlattice
Etch SiGe away
fill with gate
6–7 · Channels released, gate wraps all around
Teal = Si channel · Amber = SiGe (sacrificial) · Copper = gate · Light grey = inner spacers
Notes: Left: the superlattice as grown. Right: after channel release and replacement metal gate. The inner spacers isolate the gate from source and drain between the sheets.

## Slide 13: Eight steps; three of them are the hard part
1
Superlattice epi
2
Pattern fins
3
Dummy gate + spacers
4
Inner spacers
5
Source/drain epi
6
Channel release
7
Gate stack (ALD)
8
Contacts + BEOL
Highlighted: lateral SiGe recess to nm control, selective SiGe removal, and fitting high-k + work-function metals into ~10 nm gaps (this limits Vt flavours).
Notes: GAA adds many epitaxy, selective etch, ALD and metrology steps. That is why equipment makers such as Applied Materials, Lam, Tokyo Electron, ASM International and KLA call GAA a growth driver.

## Slide 14: Backside power: signals on top, power underneath
Signal + power wiring
Transistors
Silicon substrate
Traditional
Carrier wafer
Signal wiring only
Transistors
Power network
Backside power
Gains
Lower IR drop · more routing tracks · higher density and clock for power-hungry AI chips
Costs
Wafer bonding and thinning · nano-TSVs · worse hotspots · new debug, PDK and EDA flows
Notes: Intel PowerVia ships with 18A using nano-TSVs. TSMC Super Power Rail arrives with A16 using direct backside contacts. For physical designers: new power-grid design, IR and EM sign-off, and thermal analysis.

## Slide 15: The 2nm-class race to watch
Company | Node | Transistor | Backside power | Watch for
TSMC | N2 → A16 | Nanosheet | Super Power Rail (A16) | Volume ramp; Apple and HPC first
Intel | 18A | RibbonFET | PowerVia (first) | Can Intel Foundry win outside customers?
Samsung | SF3 → SF2 | MBCFET (first GAA, 2022) | Planned (SF2Z) | Yield and customer wins
Don’t compare names: compare density, perf/W, SRAM cell area, yield and wafer price.
Notes: TSMC N2 ramps 2025-2026 with A16 adding backside power. Intel 18A combines RibbonFET and PowerVia. Samsung was first to GAA but has struggled on yield and customer wins.

## Slide 16: Why this matters for you
Career: design and AI hardware
Roles at the process–design boundary are growing:
• Standard-cell library design and characterisation
• DTCO engineering
• PDK and EDA flow development
• IR/EM, thermal and power-integrity sign-off
Much of this work happens in Indian design centres.
Investing: who gains
• Foundries: higher wafer prices at the leading edge
• Equipment: more epi, etch, ALD, metrology steps (AMAT, Lam, TEL, KLA)
• EDA: more complex sign-off (Synopsys, Cadence)
Key risk: a slow or low-yield ramp hits margins and customer launches.
Notes: Tie the technology to roles and to where value flows. Not investment advice.

## Slide 17: Five things to remember
1
Node names are brands: compare pitches, density, SRAM, cost
2
Density now comes mostly from DTCO, not from shrinking pitches
3
More gate around the channel = better control = lower VDD
4
Nanosheets: inner spacers, channel release and gate fill are the hard steps
5
Backside power frees routing and cuts IR drop, but adds thermal and flow work
Next: exercises + quiz in notes/week-01 · Listen to the Week 1 podcast
Notes: Recap. Then do the exercises and quiz, and listen to the podcast episode for the same ideas in conversation.